TECHNICAL DATA SHEET

Closed Cell Silicone Sponge Rubber Medium Density

Sheeting Grade: AMS-3195 Smooth Finish

ASTM D-1056 Type 2

MIL-R-46089

Temperature Range: -103(F to +450(F

SPECIFICATIONS

SAE AMS-3195E Sponge, Silicone Rubber Closed Cell, Medium. These products meet the flammability requirements of FAR 25/JAR 25/CS 25 Appendix F, Part 1, (a)(1)(iv) and (a)(1)(v) horizontal flammability tests.

Automotive Standard PART 571FMVSS302

GENERAL CHARACTERISTICS FOR SILICONE RUBBER

Limiting Oxygen Index   23.2 %  BS 2872 Part 1 Radiation Resistance	>105 Grays (107 Rads) typical

Environmental Resistance Silicone rubber products have excellent resistance to ozone, oxidation, ultraviolet light, corona discharge, cosmic radiation, ionizing radiation and weathering in general. Silicone rubber products produce very low levels of toxic fume when burnt.

| Property | AMS-3195 Typical | Test Method |
| --- | --- | --- |
| Density (lb.ft-3) Compression Deflection PSI Elongation to Failure Compression Set 50 (%) 22 hours @212(F Water Absorption % Temperature ((F) Thermal Conductivity | 29 pcf 11 psi 150% 25% <3% -100° to +500° 6.4x102 Wm-1.K-1 | ASTM D 3574 ASTM D 1056 ASTM D 412 ASTM D 746 ASTM D 1056 ASTM D 746 |

*0.5” sample.                            Test Reports are available for full rolls only, and must be requested

*0.126” sample                         at order placement with c of c.  Additional charges may apply.

www.stigallindustrial.com

13

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391