TECHNICAL DATA SHEET

Closed Cell Silicone Sponge Rubber Medium Density

Sheeting Grade: AMS-3195 Fabric Finish

ASTM D-1056 Type 2

MIL-R-46089

Temperature Range: -103(F to +450(F

SPECIFICATIONS

SAE AMS-3195E Sponge, Silicone Rubber Closed Cell, Medium. These products meet the flammability requirements of FAR 25/JAR 25/CS 25 Appendix F, Part 1, (a)(1)(iv) and (a)(1)(v) horizontal flammability tests.

Automotive Standard PART 571FMVSS302.  All fabric finish material will be supplied with full test reports upon request as called out in AMS-3195 Specification.  Does not apply to cut pieces.

Environmental Resistance Silicone rubber products have excellent resistance to ozone, oxidation, ultraviolet light, corona discharge, cosmic radiation, ionizing radiation and weathering in general. Silicone rubber products produce very low levels of toxic fume when burnt.

| Property | AMS-3195 Typical Results | Test Method |
| --- | --- | --- |
| Density (lb.ft-3) Compression Deflection PSI Elongation to Failure Compression Set 50 (%) 22 hours @212(F Temperature ((F) Low Temperature Brittleness | 32 pcf 9 psi 230% 3.5% -96° to +500° -96° | ASTM D 1056 ASTM D 1056 ASTM D 412 ASTM D 1056 ASTM D 2137 ASTM D2137 |

*0.5” sample.                Test Reports are available for full rolls only. Testing must be requested

*0.126” sample             at order placement with c of c.  Additional charges may apply.

www.stigallindustrial.com

15

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391