TECHNICAL DATA SHEET

Closed Cell Silicone Sponge Rubber Firm Density

Sheeting Grade: AMS-3196 Firm Fabric Finish

ASTM D-1056 Type 2

MIL-R-46089

MIL-R-6130 Type 2 Grade B & C Firm

Temperature Range: -103(F to +450(F

SPECIFICATIONS

SAE AMS-3196 Sponge, Silicone Rubber Closed Cell, Firm. These products meet the flammability requirements of FAR 25/JAR 25/CS 25 Appendix F, Part 1, (a)(1)(iv) and (a)(1)(v) horizontal flammability tests.

Automotive Standard PART 571FMVSS302

GENERAL CHARACTERISTICS FOR SILICONE RUBBER

Limiting Oxygen Index   23.2 %  BS 2872 Part 1 Radiation Resistance	>105 Grays (107 Rads) typical

Environmental Resistance Silicone rubber products have excellent resistance to ozone, oxidation, ultraviolet light, corona discharge, cosmic radiation, ionizing radiation and weathering in general. Silicone rubber products produce very low levels of toxic fume when burnt.

| Property | AMS-3196 Typical | Test Method |
| --- | --- | --- |
| Density (lb.ft-3) Pounds / cubic foot Compression Deflection PSI Elongation to Failure Compression Set 50 (%) 22 hours @212(F Water Absorption % Temperature ((F) | < .25” thick 52 pcf ≥ .25” thick 43 pcf 12-20 psi 200% 60% max <5% -67°F to +500°F | ASTM D 1056 ASTM D 1056 ASTM D 412 ASTM D 1056 ASTM D 746 ASTM D 746 |

*0.5” sample

*0.126” sample				www.stigallindustrial.com

17

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391