Product:    VIT-1060

Description: VIT-1060 is compounded  to offer premium performance with a competitive price.  These products are formulated for gasket sealing.

VIT-1060 is the most commonly use Fluoroelastomer sheet by the      industrial gasket supplier.

Product Type:  “A”                             		  Fluorine: 66%

ASTM: D2000M5HK710A1-10B38Z1

Z1=60 Shore A

Not recommended for:  service in acids, steam, hot water, low molecular weight esters & ketones, certain amines, hot anhydrous hydrofluoric or chlosulphonic acids and alkyl phosphate esters.

Typical Physical Properties

| Durometer (Shore A) Hardness | 60 +/-5 |
| --- | --- |
| Tensile Strength (psi) | 1200 |
| Elongation at Break (%) | 250 |
| Specific Gravity | 1.89 |
| Temperature Rating (operating) | -20°F to +400°F |
| Color | Black |

*Physical properties shown were obtained on a molded .080” thick ASTM sample

These properties are typical results, and should not be used to set quality control specifications.

Proudly Manufactured in the USA

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391