Product Specification Sheet

Product #: VIT-1775  (Aflas®)

Description:  75 durometer Aflas® TFEP  compound offers excellent resistance to high pH lubricants, greases, & coolants, drilling muds, steam, hot water, amines and phosphate esters.  VIT-1775 is offers exceptional fluid resistance to strong bases.

Product Type:  “TFEP”                         Fluorine: ~56%

Cure System:  Peroxide  	     Polymer: TFEP Tetrafluoraethylene and

propylene

Not recommended for: Temperatures above +400° F Continuous

Typical Physical Properties

| Durometer (Shore A) Hardness | 75 +/-5 |
| --- | --- |
| Tensile Strength (psi) | 2550 |
| Elongation at Break (%) | 180% |
| Modulus at 100% Elongation (psi) |  |
| Specific Gravity | 1.62 |
| Compression Set (%) 22 hrs @ 350°F | 30% |
| Temperature Rating (operating) | -10°F to +400°F |
| Color | Black |

*Physical properties shown were obtained on a molded .080” thick ASTM sample

These properties are typical results, and should not be used to set quality control specifications.

Updated 6-2018

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391