Viton™ SPONGE RUBBER SHEET

Low Density Skin on Both Sides

Product Specification Sheet

Product:	VIT-1028

Description: Closed Cell Viton™ sponge formulation with continuous skin on both sides.  Like solid FKM sheet, VIT-1028 is generally resistant to alphalitic and aromatic hydrocarbons, oil, fuels, ozone, and weather, and lubricants.  The sheet provides excellent lightweight thermal insulation.

Product Type: “A”   66% Fluorine		     		Temp Range: -10F to +400F

| Thickness | 1/8” | ¼” | 3/8” | 1/2” |
| --- | --- | --- | --- | --- |
| Water Pick Up (%) wt. Increase | 0% | .02% | .06% | .01% |
| Compression Set % |  |  |  |  |
| 22 hrs @ 75F | 27% | 13% | 14% | 17% |
| 22 hrs @ 158F | 100% | 100% | 100% | 100% |
| Low Temp Brittleness | -10F | -10F | -10F | -10F |
| Compression Deflection (PSI) |  |  |  |  |
| 25% Deflection – Original | 6.5% | 5.5% | 4.0% | 3.5% |
| Density – LBS / CF | 19 | 17 | 15 | 10 |
| Thickness Tolerance | + .050” -.030” | + .060” -.060” | + .080” -.080” | + .125” - .125” |

*Physical properties shown were obtained on a molded .080”thick ASTM sample

These properties are typical results, and should not be used to set quality control specifications.

www.stigallindustrial.com

It is the end users responsibility to determine the all elastomers fitness for use.

The word Viton™ is a registered trade mark of The Chemours® Company

Prices are subject to change without notice.

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391