Product Specification Sheet

Product#: F-1375

Description:  75 durometer Acid Resistant intermediate fluorine, Fluoroelastomer compound.  Compound offers excellent resistance to strong mineral acids,  chlorinated solvents, aliphatic & aromatic hydrocarbons, fuels, oils, lubricants, UV light and ozone.

Product Type:  “B”                               Fluorine: 68%

Cure System:  Bisphanol 	                   Polymer: Terpolymer of VF2/HFP/TFE

ASTM: D2000 M5HK710B38Z1

Z1= 75 Shore A

Not recommended for: low molecular weight esters, ketones, amines, hot anhydrous hydrofluoric or chlorosulphonic acids, & alkyl phosphate esters.

Typical Physical Properties

| Durometer (Shore A) Hardness | 75 +/-5 |
| --- | --- |
| Tensile Strength (psi) | 1800 |
| Elongation at Break (%) | 250% |
| Modulus at 100% Elongation (psi) | 350 |
| Specific Gravity | 1.87 |
| Temperature Rating (operating) | -20°F to +450°F |
| Color | Black |

*Physical properties shown were obtained on a molded .080” thick ASTM sample

These properties are typical results, and should not be used to set quality control specifications.

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391