Viton™ “GF” SHEET PRICING

Proudly manufactured in the USA

Description:  VIT-1475  Viton™ GF is compounded offers excellent resistance to

oxygenated fuels such as MTBE and MeOH, strong mineral acids, chlorinated

solvents, aliphatic & aromatic hydrocarbons, fuels, oils, lubricants, UV light,

ozone, steam and hot water. Manufactured with 100% Virgin Viton™ by the

Chemours® Company.

Product Type:  “GF”                               	  Fluorine: 70%

Cure System:  Peroxide  	    	   	  Polymer: Terpolymer of VF2/HFP/TFE

Not recommended for: low molecular weight esters, ketones, amines, hot anhydrous hydrofluoric or chlorosulphonic acids, & alkyl phosphate esters.

Typical Physical Properties

| Durometer (Shore A) Hardness | 75+/-5 |
| --- | --- |
| Tensile Strength (psi) | 1450 min |
| Elongation | 150% min |
| Temperature Rating (operating) | -20(F to +450(F |
| Compression Set -22 hrs @392F % of Original Deflection ASTM D395 | 15% Max |
| Specific Gravity | 1.87+/-.03 |
| Finish | Smoot or Satin |
| Color | Black |

Physical Properties shown were obtained on a molded .080” ASTM Sample.   These are typical results.

www.stigallindustrial.com

It is the end users responsibility to determine the elastomers fitness for use.

The word Viton™is a registered trademark of the Chemours® Company

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391