Product Specification Sheet

Product #: F-1675  (Viton Extreme®)

Description:  75 durometer Fluoroelastomer (ETP) compound offers excellent resistance to high pH lubricants, greases, & coolants, drilling muds, sour wells solvents, coatings, and ultra harsh environments.  This polymer is supplied by Dupont Performance Elastomers Inc.

Product Type:  “ETP®”                       Fluorine: ~67%

Cure System:  Peroxide  	Polymer: Copolymers of TFE/Propylene and                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                                               Ethylene/TFE/PMVE

ASTM: M2HK714 A1-10, B38,C12,EF31, E078, Z1Z1 = 75 +/- 5 DURO

Typical Physical Properties

| Durometer (Shore A) Hardness | 75 +/-5 |
| --- | --- |
| Tensile Strength (psi) | 2000 |
| Elongation at Break (%) | 150 |
| Specific Gravity | 1.83 |
| Compression Set (%) 22 hrs @ 350°F | 50 |
| Temperature Rating (operating) | -10°F to +400°F |
| Color | Black |

*Physical properties shown were obtained on a molded .080” thick ASTM sample

These properties are typical results, and should not be used to set quality control specifications.

Up dated 01.15

# Text boxes

Box 1228

Sealy, TX 77474

TEL (979) 885-2241

FAX (979) 885-7391